Beryllium Acceptors in III-Nitride Semiconductors: Final Report

Prepared by

## Chris G. Van de Walle, Xerox Palo Alto Research Center

For the

# Office of Naval Research, Contract # N00014-99-C-0161
Program Officer: Dr. Colin Wood

# Contributors:

# Chris G. Van de Walle, Sukit Limpijumnong, John E. Northrup, Linda T. Romano, Michael Kneissl, Peter Kiesel, and Noble M. Johnson, Xerox PARC

# Thomas H. Myers and A. Ptak, West Virginia University

## Summary

## The purpose of this program was to assess the potential of beryllium (Be) as a p-type dopant in GaN. The program involved both computational and experimental studies.  Growth was carried out by molecular beam epitaxy (MBE), and structural (TEM, Auger, and SIMS), electrical (resistivity and Hall measurements), and optical (PL) characterization was performed.  First principles calculations highlighted the promise of Be, and addressed some of the potential problems.

## At the conclusion of this one-year program, we can report that we succeeded in incorporating Be in GaN in high concentrations; we learned from structural studies what the optimal growth conditions are; we verified, in photoluminescence, the presence of Be acceptors; and we observed the presence of p-type conductivity in Hall measurements.  The latter, however, also revealed the presence of significant compensation.  Our calculational work has indicated that compensation by Be interstitials can be an important problem; these studies also provide guidelines for suppressing compensation and/or removing compensating center in post-growth treatments. We are therefore in an ideal position to overcome the remaining obstacles and fully realize the potential of Be doping, should a continuation of this program be approved.

Experimental Studies

Details of Growth

The GaN layers for this study were grown at West Virginia University by molecular beam epitaxy (MBE) in a custom system.  A standard MBE source provided the Ga flux.  An rf-plasma source was used to produce active nitrogen (EPI Vacuum Products Unibulb).  Atomic hydrogen was produced using a thermal cracker (EPI-AHS) operating to give an atomic hydrogen flux of one monolayer-equivalent every 1-3 s.  High purity Be (99.999%, Atomergics Chemetals Corporation) was evaporated from a dopant effusion cell (EPI-5-D).

A total of forty-two growths were performed on this contract.  The initial eight were to assess the difference in growth kinetics between the Ga-polar and N-polar faces.  The next ten were used to investigate Mg-doping to set a baseline in p-type doping for comparison with subsequent studies with Be, with the final twenty-four investigating Be doping.  Of the Be-doped samples, six have been grown to study incorporation kinetics and the remainder uniformly doped.  Unfortunately, the last eight Be-doped growths were of poor quality due to a bad batch of sapphire.  Selected samples from all sets were sent to Xerox for additional characterization.

Initial growths focused on developing a reasonable procedure for preparing clean GaN surfaces suitable for subsequent growth of GaN by MBE in order to use the MOCVD-GaN templates provided by Xerox.  As part of this effort, we have investigated, to some extent, the differences in growth kinetics between Ga-polarity (MOCVD template) and N-polarity (MBE on sapphire) orientations.  In particular, growth on the Ga-polarity requires a significantly larger Ga-overpressure to produce two-dimensional growth conditions.

Mg Incorporation Experiments

The general conclusions listed in the second quarter report remain valid.  In summary: (1) we always observed an increasing incorporation of Mg in the GaN with increasing Mg oven temperature, that is, we did not observe a saturation previously reported by others [1]; (2) there is a significant difference in Mg incorporation depending on polarity with the Ga-polarity incorporating a factor of up to thirty times more Mg than the N-polarity under the Ga-rich growth conditions used; (3) only a small fraction of the actual Mg flux is incorporated; (4) there is a very strong substrate temperature dependence on Mg incorporation; (5) there is a distinct increase in Mg incorporation in the presence of atomic hydrogen; and (6) there is also an indication that a surface-accumulation layer of Mg may be forming during doping.

A final important point is that a dramatic decrease in Mg incorporation (as determined by SIMS) was observed for Ga-polarity GaN when the Mg flux was increased to produce a monolayer/sec flux on the surface.  The incorporation after this abrupt decrease was more consistent with that observed for the N-polarity.  The observed change in incorporation is highly suggestive of surface inversion, changing from Ga-polarity to N-polarity.  This has been verified by TEM [2].  The observed polarity inversion is consistent with the prior results of Ramachandran et al. [3]  Such a surface inversion, coupled with the concomitant decrease in Mg incorporation, represents a potentially serious issue with heavy Mg-doping of GaN by MBE at higher growth temperatures.

Be Incorporation Studies

Six samples were grown and analyzed by SIMS to specifically study Be-incorporation kinetics.  The effect of atomic hydrogen on incorporation was also studied.  Three of the SIMS measurements on these samples are shown in Figures 1-3.   As indicated in Fig. 1, at low concentrations the Be incorporation profile appears to be that expected for classic surface accumulation/segregation.  While diffusion effects are undoubtedly present as well, the pronounced lack of any step-like structure relating to the opening and closing of the Be shutter is consistent with surface accumulation.  Again, similar to the Mg case, the presence of atomic hydrogen enhances incorporation at low fluxes and sharpens the profiles at higher fluxes.  There also seems to be a significant substrate temperature dependence on incorporation at lower flux.

Figure 1.  Be incorporation in Ga-polarity GaN as a function of various substrate and oven temperatures.  The opening and closing of the Be shutter is shown schematically, with the magnitude changes merely to suggest increases and decreases in Be flux without being quantitatively correct.

Figure 2 shows a similar growth sequence for N-polarity growth.  Two traces are shown.  On this sample, the location of the RHEED beam during growth was discernible.  While there was a small effect on maximum incorporation of Be, the presence of the high energy electrons greatly sharpened the profiles.  We interpret this as due to enhanced Be desorption, possibly related to an electron stimulated desorption effect.  Again, this is consistent with the presence of a Be-accumulation layer on the surface.

Figure 2.  Be incorporation in N-polarity GaN as a function of various substrate and oven temperatures.  The opening and closing of the Be shutter is shown schematically, with the magnitude changes merely to suggest increases and decreases in Be flux without being quantitatively correct.  The location of the area exposed to electron irradiation during RHEED was discernible on this sample.  The black trace represents the Be-incorporation under this electron irradiation, while the red trace represents incorporation without electron irradiation.

Figure 3 shows the SIMS results for Ga-polarity GaN for higher concentrations of Be.  Again, the profiles were offset with respect to the opening and closing of the dopant shutter, consistent with surface accumulation.  Unlike the low concentration case, atomic hydrogen did not seem to influence Be incorporation.  The small decrease merely reflects the increase in GaN growth rate that occurs in the presence of atomic hydrogen.  Atomic hydrogen was not observed to significantly change Be incorporation for any N-polarity samples investigated.  In general, there seemed to be a larger incorporation of Be on N-polarity GaN with little discernible difference in incorporation due to atomic hydrogen.   Although not shown, additional SIMS indicated that Be incorporation at higher flux is typically a factor of two larger on N-polarity than Ga-polarity for the same Be flux; that unlike Mg, incorporation is not a strong function of temperature at higher concentrations although some temperature dependence is present at low concentrations; and incorporation rates do not change significantly (~25% increase) when going from very Ga-rich growth conditions to N-stable growth.

Figure 3.  Be incorporation in Ga-polarity GaN as a function of various substrate and oven temperatures.  The opening and closing of the Be shutter is shown schematically, with the magnitude changes merely to suggest increases and decreases in Be flux without being quantitatively correct.

In addition to the Be-profile shapes, most of the SIMS measurements were also suggestive of a higher concentration of Be at the surface.  Auger measurements were made on several step-doped and uniformly doped layers.  Although quantitative interpretation was complicated, the presence of Be was measured to be at levels representing a significant fraction of a monolayer.  As discussed later, this surface layer may have a significant influence on the as-grown properties.

SIMS measurements made on the Be-doped samples indicated a low background for both oxygen and carbon, less than the background (low-to-mid 1016 cm-3) for these measurements.  Measurements also indicate that hydrogen is incorporated at levels at or above the Be concentration when grown under atomic H.  An increase in the background oxygen and carbon was also observed for growth under atomic H; the origin of this effect needs further investigation.

In summary, Be incorporation in GaN grown by rf plasma MBE is much better behaved than Mg, showing significantly less dependence on growth conditions.  Strong evidence was observed for surface accumulation of Be during growth.  Atomic hydrogen only seemed to significantly affect incorporation at low Be concentrations on Ga-polarity material.

Figure 4a. TEM image of GaN:Be

Figure 4b. High magnification TEM image of upper defect layer shown in Fig. 4a.

Structural Characterization with Transmission Electron Microscopy (TEM)

Figure 5a. High resolution TEM image of inversion domain in GaN:Be.

Figure 5b. Inversion domains in MOCVD grown GaN:Mg [Ref. 3].

Samples grown with different Be concentrations were investigated by TEM at Xerox PARC. Figure 4 is a TEM image of a step-doped GaN film grown by MBE on a Ga-polarity MOCVD template (sample #15). The corresponding SIMS profile of the Be concentration is shown in Fig. 3.  Figure 4 shows that the threading dislocations (TD) initiated in the MOCVD film changed line direction when Be was incorporated (Layer 1 in Fig. 4a).  According to the SIMS profile, this occurred within the first doped layer at a Be concentration [Be]  ~ 1017cm-3.   At a depth of ~ 2.5 m from the surface, a second interface was observed (layer 2) corresponding to [Be] ~ 5 x 1019cm-3. Cracks were also occasionally observed within layer 2. A higher magnification of layer 2 is shown in Fig. 4b.  It is observed that this layer consists of a high density of inversion domains that extend along the growth direction. The domains range in width from ~ 10-100 nm.	A high resolution TEM image of a single inversion domain is shown in Fig. 5a. The shape of the inversion domain (ID) is similar to inversion domains that formed in MOCVD GaN films with a Mg concentration of  ~ 2 x 1020cm-3 as shown in Fig. 5b [3].

Photoluminescence Characterization

Room temperature UV fluorescence measurements indicate that the samples are uniform, but with one striking difference.  The Be-doped layers fluoresce orange in color, except for those that were grown under atomic hydrogen.  These do not have the orange color, but appear to be more of a mixture of blue and yellow.  While qualitative, this indicates a significant difference between the layers grown with and without atomic hydrogen.

Figure 6 shows a low-temperature photoluminescence spectrum from one of the Be-doped GaN layers.  All Be-doped GaN exhibited a strong feature near 3.38 eV, which is the most prominent feature for most samples.  Temperature and power dependence studies consistently indicate that this is donor-acceptor pair luminescence.  Previous studies of Be-doped GaN have also reported the same feature with a similar interpretation [4].  Using the typical shallow donor energy in GaN of 20 to 35 meV, this would indicate an acceptor ionization level at about 100 meV.  The previously unreported feature at 3.397 eV was observed on two of the N-polarity samples, and has temperature and power characteristics of an electron-acceptor transition. The transition lineshape obtained using weak below-gap illumination was consistent with this interpretation.  Again, this would indicate an acceptor level ~ 100 to 110 meV above the valence band.  The feature at 3.472 eV is tentatively assigned to an acceptor-bound exciton with a binding energy of 8 to 8.5 meV.  This low binding energy is again consistent with Be as a shallow acceptor.

Figure 6.  Low temperature photoluminescence of a Be-doped GaN sample.

The feature at 3.27 eV has also been previously reported for Be-doped material and also has donor-acceptor pair characteristics [5]. There is also a transition near 3.138 eV near what has previously been labeled the I4 transition.  Interestingly, these latter two features were removed after etching the surface of the GaN, indicating they may be related to the surface accumulation layer.  Samples grown under atomic hydrogen did not exhibit any of the above acceptor-related features.  Instead, there was a single sharp peak at 3.477 to 3.479 eV that did not have associated phonon replicas, more indicative of a donor bound exciton.

Electrical Characterization

Eight uniformly Be-doped layers have undergone electrical characterization at West Virginia University.  A subset of these layers, as well as two step-doped structures, were also characterized at Xerox PARC.

Initial Hall measurements at WVU using In contacts were not successful because the contacts were highly rectifying.  Pt contacts sputtered on the Be-doped GaN proved to be ohmic.  Room temperature Hall measurements of the as-grown samples indicated n-type conductivity.  Interestingly, samples containing evidence of a RHEED stripe exhibited about a factor of 300 anisotropy in resistivity when comparing measurements perpendicular and parallel to the stripe.  The Hall measurements were also extremely sensitive to the current in the sample.  We took this as an indication that the surface accumulation of Be was having an effect on the Hall measurement, and etched the surface with aqua regia in an attempt to remove this layer.  The process was non-optimal as it left a very rough surface.  Pt contacts deposited on this surface were initially ohmic, but degraded after a period of days.  Room temperature measurements made at WVU on samples treated in this fashion indicated weak p-type conduction with carrier concentrations ranging from low 1015 to high 1016 cm-3.  Layer resistivities ranged from 4 to 100 -cm.

Hall measurements performed at Xerox confirm that the results depend strongly on the current.  Ohmic contacts are difficult to obtain, and show significant variations across the sample.  These issues could be related to structural problems near the surface, or to laterally varying compensation.

The most consistent results were obtained for a step-doped structure (sample #18, with a profile similar to sample #15 shown in Fig. 3).  Chemically assisted ion-beam etching (CAIBE) was used to etch away the first 2 m, thus exposing a region which, from SIMS, has a high Be concentration (2 x 1018 cm-3) and, from TEM, has good structural quality.  This sample showed clear p-type behavior in more than 30 measurements.  However, probably due to the non-Ohmic nature of the contacts, strong variations in hole concentration and mobility were obtained (mobility values between 2…100 cm2/Vs, concentrations between 0.2…3 x 1017 cm-3, assuming a 1 m thick homogeneously doped layer).  Temperature-dependent Hall measurements on this sample indicated conductance with an activation energy of 150 meV for temperatures above 360 K, and mobilities around 10 cm2/Vs, decreasing at higher temperatures.  However, these results are not definitive since they could not be reproduced in subsequent measurements.

At this point the main conclusion is that some of the Be-doped samples show distinct signs of p-type conductivity, but a number of issues need to be addressed, including the formation of Ohmic contacts, the homogeneity of the layers, and the presence of compensation.

Theory

Overview

In the course of this contract, we performed extensive first-principles calculations and analysis of the interaction of Be impurities with GaN.  We studied the structural and electronic properties of Be in substitutional and interstitial positions, in the bulk as well as on the surface.  Beryllium interstitials act as donors, and therefore compensate the intended p-type conductivity; we therefore studied their formation and migration in great detail.  A tendency for neutral BeGa to move off the substitutional site was observed; the ionization energy, however, was not affected. We calculated formation energies, which provide direct information about solubilities and potential compensation.  Incorporation of Be in the zinc-blende vs. the wurtzite phase was explicitly compared; the properties were similar, with a somewhat higher risk of compensation due to Be interstitials in the zinc-blende phase.  We studied the formation of Be-H complexes, finding a larger binding energy than for Mg-H.  And we investigated Be-O-Be complexes, concluding that co-doping with oxygen will not offer any benefits.

For details about these various investigations, we refer to the quarterly reports and to the publications which have already been submitted or are in preparation.  In this final report we focus on results obtained during the final quarter of the contract.

Polarity inversion caused by acceptor dopants at high concentrations

Studies of Mg doping of GaN have shown that the incorporation of high levels of Mg is often accompanied by the formation of extended defects. In MBE, exposure of the (0001) surface to ~ 1 ML of Mg can cause an inversion of polarity from Ga-face to N-face.  TEM images have also revealed the presence of inverted regions in Mg-doped layers of films grown by MOCVD [3].

Under the current ONR contract we have employed transmission electron microscopy, convergent beam electron diffraction, secondary ion mass spectrometry, and first-principles total energy calculations to investigate the microstructure of Mg-doped GaN films grown by rf-plasma MBE [2].  We have observed that a sufficiently high Mg concentration on the (0001) growth surface of GaN triggers an instability with respect to polarity inversion, with the formation of a multifaceted inversion domain boundary (IDB).   TEM shows that the IDB is faceted predominantly along the {0001} and  {h,h,-2h,l} planes, with l/h  approximately equal to 3. Using first-principles total energy calculations we have shown that (1122) and (1123) IDBs are stabilized by the incorporation of Mg in threefold coordinated lattice sites at the boundary. This is evidence that heavy Mg-doping drives the formation of these planar defect structures.  The formation of Mg-rich IDBs in GaN causes electrical deactivation of Mg and appears to be an important mechanism limiting the p-type doping of GaN.  A paper [2] describing our investigations in detail been submitted to Applied Physics Letters, and a preprint is included as an appendix to this report.

Optimizing Be incorporation during growth

We suggest two possible means of enhancing incorporation of Be on the substitutional site. The proposals are predicated on the assumption that the bulk concentration of BeGa depends, to some extent, on the concentration of BeGa at the surface during growth. Thus, to increase our understanding of dopant incorporation in molecular beam epitaxial growth, it may be useful to consider the formation energy of a dopant as part of the surface reconstruction that is present during the growth.

Ga

N

Ga (T1)

Ga adlayers

BeGa

Ga (S3)



Ga (T4)

(a) Be substitutional

Ga

N

Be interstitial

Ga adlayers

(b) Be interstitial

Figure 7. Schematic model of a reconstruction of the GaN(0001) surface in which a bilayer (i.e., two adlayers) of Ga is present. (a) In this structure a Be atom is incorporated on the Ga site in the S3 layer (layer 2). The Be-N bond lengths are 1.65 Å and   is 0.13 Å. (b) A Be interstitial is located just below the surface. The Be-N bond lengths are 1.60 Å and  is -0.20 Å.

On the basis of total energy calculations we propose that it may be possible to enhance the BeGa incorporation probability relative to incorporation as an interstitial by employing a Ga-rich (0001) growth surface in which a metallic bilayer of Ga is present on the surface [6,7] This metallic layer pins the Fermi level ~0.7 eV above the bulk valence band maximum, and this electron-rich environment favors incorporation of substitutional acceptors at the surface. Under these conditions the incorporation at the surface of a BeGa is energetically favorable with respect to an interstitial Be by about 1.0 eV.

Our calculations also indicate that the use of indium to create a compressively strained surface [8,9] layer may promote the co-incorporation of Be on the substitutional site. Because Be is much smaller than the Ga atom it replaces, Be incorporation compensates the compressive stress caused by the In.  The formation energy of BeGa on an In-rich surface is lower than that for an In-free surface by about 0.8 eV. This suggests the possibility of using In as a surfactant to promote Be incorporation, and vice versa.

(a) {4/4} In adlayer

(b) {7/4} In adlayer

Ga

N

In

BeGa

Ga

Ga

N

In

BeGa

In

Figure 8. Schematic model of GaN(0001):In surfaces. (a) The {4/4} structure. (b) The {7/4} structure.

These proposals are based on total energy calculations for Be atoms in various configurations on the GaN (0001) surface. To model the reconstructions that occur under the Ga-rich conditions that are optimal for growth on the (0001) surface, we employ a model having two adlayers of Ga as shown in Fig. 7. This model is very similar to the laterally contracted Ga bilayer reconstruction that exists on the surface following MBE [6,7].  The equilibrium geometries were determined by energy minimization. In Fig. 7(a) the Be atom substitutes for a Ga atom in the S3 site, where it forms three bonds with N atoms. In Fig. 7(b) the Be is located in an interstitial site just below the surface.  We calculate that the substitutional site is lower than the interstitial site by at least 1.02 eV; i.e., a reaction in which a Be interstitial replaces a Ga atom and the removed Ga atom is placed in a bulk Ga reservoir is exothermic by 1.02 eV. The exothermicity of this reaction will tend to suppress the concentration of Be interstitials at the surface with respect to the number of Be atoms in substitutional sites.

We turn now to the study of Be incorporation on the In-terminated surface. Previous theoretical and experimental work has shown that it is possible to form a surface structure in which there is one monolayer of In atoms in atop sites as shown in Fig. 8(a) [8,9]. It is also possible to create a surface in which some of the Ga atoms in the S3 layer are replaced by In, as indicated in Fig. 8(b). This replacement results in compressive stress because the In atom is larger than the Ga atom that it replaces. There is a limit to the amount of In that can be incorporated in the S3 layer before stress-relieving nanostructures form spontaneously [8]. Here we suggest that this compressive stress may also be relieved by incorporation of Be in the S3 layer, and this could lead to an enhancement in the Be doping concentration.

Calculations were performed to determine the formation energy of Be on these two In-terminated surfaces. We refer to these structures, which have 22 symmetry, in terms of the amount of indium that is present. The {4/4} structure contains 1 ML of In atoms located in the atop sites shown in Fig. 8(a). The {7/4} structure contains 7/4 ML of In atoms, ¾ of which are located in the S3 layer defined in Fig. 8(b). The energy to replace a Ga atom in the S3 layer with a Be atom was calculated for both structures. The calculated Be-N bond length is noticeably shorter in the {7/4} structure, a consequence of stress compensation.  For the same Be and Ga chemical potentials the energy of incorporation on the {7/4} surface is lower by 0.8 eV. The difference in the energy arises because of the stress compensation that occurs in the {7/4} structure: it is much more favorable to incorporate the Be on the In-rich surface.

In conclusion, we have analyzed the energy of Be incorporation on the GaN(0001) surface. We have identified two mechanisms; metallic surface reconstructions and compressively strained surfaces, that may be useful to enhance the incorporation of Be on the Ga sublattice.

Diffusion of Be interstitials

Figure 9. Formation energies of various configurations of Be in wurtzite GaN under N-rich conditions.

During the final quarter of our contract we have finalized our studies of Be interstitials.  As illustrated in Fig. 9, Be interstitials have formation energies comparable to substitutional acceptors; it is therefore likely that they will be incorporated during growth, and compensate the intended p-type doping. We performed a comprehensive study of the total energy surface, describing the motion of Be interstitials through the lattice.  The diffusion barriers turn out to be highly anisotropic, with diffusion parallel to the c-axis exhibiting a relatively high barrier of 2.9 eV, while diffusion in planes perpendicular to the c-axis can proceed with a barrier of 0.9 eV.  These features of the Be total-energy surface are strikingly illustrated in the contour plot (Fig. 10a) and perspective plot  (Fig. 10b).

During the fourth quarter, we have also investigated the complex consisting of a Be interstitial bound to a substitutional Be acceptor.  Such a complex is likely to form, since the interstitial donors and substitutional acceptor are coulombically attracted.  The mobility of the interstitials will also enable them to search out and bind to the acceptors.  We have calculated a binding energy of 1.3 for this complex; the formation energy of the complex is included in Fig. 9.  This binding energy would need to be added to the diffusion barrier in order to arrive at the activation energy for removing Be from the p-type layer.  The process of activation will therefore consist of first dissociating the Beint-BeGa complex, and then diffusing the Beint through the layer; with diffusion barriers of 2.9 eV parallel to the c-axis, and 0.9 eV perpendicular to the c-axis.   A manuscript detailing these findings is in preparation.

Finally, we have continued our investigations of Be-H complexes by calculating the vibrational frequency of the stretching and wagging modes in this complex; they are 3350 cm-1 and 650 cm-1, respectively.  The frequency of the stretch mode is close to vibrational frequencies in NH3 molecules, which is to be expected given the strong N-H binding that occurs in the Be-H complex.  Knowledge of these frequencies is important to aid in the experimental detection of such complexes using vibrational spectroscopy.

Figure 10.  (a) Contour plot and (b) perspective plot of the formation

energy surface for Beint in a [-1100] plane through the host atoms.  In the contour plot the contour interval is 0.5 eV and the spatial dimensions along both directions are in Å.

## Outlook

After a one-year program, we have completed all of the goals that were stated in the proposal for this program.  We have achieved a convincing demonstration of our ability to incorporate high concentration of Be in GaN.  Thanks to extensive structural studies, we have developed a thorough understanding of the effect of growth conditions on Be incorporation and structural quality of the layers.  And we have strong indications of electrical and optical activity of Be acceptors.  The results of our studies indicate that better control of homogeneity and compensation could result in good p-type conductivity; and our theoretical work has provided us with guidance as to what the sources of the compensation are, and how they may be overcome.

We are thus well positioned to pursue a continuation of this program.  Such a follow-on program would obviously address the issue of compensation and how it could be avoided; a rigorous determination of the ionization energy of the Be acceptor using temperature-dependent Hall measurements; an investigation of Ohmic contacts to Be-doped material, including a study of surface layers and etching; studies of the effect of hydrogen on Be incorporation and on compensation; and, theoretically, studies of Be in AlGaN, the effects of hydrogen on Be incorporation in GaN and AlGaN, and of the surface accumulation layers.

References

[1] S. Guha, N. A. Bojarczuk and F. Cardone, Appl. Phys. Lett. 71, 1685 (1997).

[2] L. T. Romano, J. E. Northrup, T. Myers and A. Ptak (submitted to Appl. Phys. Lett.).

[3] V. Ramachandran, R.M. Feenstra, W. L. Sarney, L. Salamanca-Riba, J. E. Northrup, L. T. Romano, D. W. Greve, Appl. Phys. Lett. 75, p.808 (1999).

[4] F.J. Sanchez, F. Calle, M. A. Sánchez-Garcia, E. Calleja, E. Munoz, C. H. Molloy, D. J. Somerford, J. J. Serrano and J. M. Blanco, Semicond. Sci. Technol. 13, 1130 (1998).

[5] A. Salvador, W. Kim, O. Atkas, A. Botchkarev, Z. Fan and H. Morkoc, Appl. Phys. Lett. 69, 2692 (1996).

[6] A. R. Smith, R. M. Feenstra, D. W. Greve, M. S. Shin, M. Skowronski, J. Neugebauer, and J. E. Northrup, J. Vac. Sci. Technol. B 16, 2242 (1998); Appl. Phys. Lett. 72, 2114 (1998).

[7] J. E. Northrup, J. Neugebauer, R. M. Feenstra, and A. R. Smith, Phys. Rev. B 61, 9932 (2000).

[8] H. Chen, R. M. Feenstra, J. E. Northrup, T. K. Zywietz, and J. Neugebauer  (submitted to Phys. Rev. Lett.).

[9] J. E. Northrup and J. Neugebauer, Phys. Rev. B 60, 8473 (1999).